## Slide 1: Spherical Microwell Arrays for Mesenchymal Stem Cell Cultures
KUO, Hsu-Ting
Supervisor: Keng-hui Lin
Institute of physics

## Slide 2: Motivation
In Lin’s lab, the former postdoc, Jonny Huang, developed a spherical microwell arrays as a novel 3D culture method.
Data shows that the self-renewal ability of REF52 cell decreases under 3D confinement
Get rid of this
40 mm
60 mm
80 mm
100 mm
Rat embryonic fibroblast REF52

## Slide 3
Step 1: Create an array of micrometric cylindrical holes on PDMS
Step 2: Manually placed glass microspheres one by one onto the cylindrical holes
Step 3: Pour fast curing silicone on PDMS
Step 4: Peel off the microspheres
Step 5: The second silicone template is applied with an off-the-shelf two-part epoxy resin and evenly appended to a glass-slide
 Step 6: Obtain monolithic epoxy microsphere mold
MOLD 1
MOLD 2
MOLD 3
Original protocol

## Slide 4
Step 7: Using the mold to make PA gel
Step 8: Sterilization process (UV light)
ECM proteins
Step 9: Protein coating on the PA gel
Step 10: Peal off extra protein
aldehyde-coated slide
overnight
top ECM removal
Pressure

## Slide 5: Drawback of the Original Protocol
Time consuming:
around 3 days
10 steps
3 different molds
involved
Labor consuming

## Slide 6: Objective
Our goal is to:
Simplify the protocol of making 3D cell cultured platform
Observe the change in self-renewal ability of mesenchymal stem cells (MSC) under 3D confinement.

## Slide 7: Simplifying steps of making the 3D cell cultured platform
Simplify the procedure of beads placing
Avoid the step of pealing off extra protein
Microspheres coating with ECM proteins

## Slide 8: Placing beads on an array of through holes
To achieve this purpose, I designed a chuck to hold the hole arrays.

## Slide 9
Making Hole Arrays
Custom-made by laser hole drilling.
2’’ si wafer
Thickness: 275um
4’’ si wafer
Thickness: 400um
5’’ si wafer
Thickness: 500um
106.67um
83.95um
113.25um
83um
52um
52um
Problem: Non-spherical holes. The vacuum leaks when the spherical spheres sit on top.

## Slide 10
Solution:
Use glue to keep beads in place
glue

## Slide 11
glue
Solution:
Use glue to keep beads in place

## Slide 12
Avoid the step of pealing off protein
glue
Cover glass
PA gel
Coat protein on beads beforehand

## Slide 13
MSC grown in 60 mm pores
2019/08/15 Day0
2019/08/19 Day3
20x TRITC Fluorescent dye: CellTracker
Single cell in pores undivided :
N: 38 out of 38  100%

## Slide 14
(a)
(b)
(c)
MSC grown in 60 mm pores
Day 0
Day 3
Day 5

## Slide 15
MSC grown in 100 mm pores
Day 0
Day 3
Day 5
(a)
(b)
(c)

## Slide 16: Conclusion
It is possible to use the new protocol to replace the old method.
We also observe the cell cycle arrest of mesenchymal stem cells in spherical microwell arrays.

## Slide 17: Questions?

## Slide 18: Thank you!